South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

MET 320	HQ 3	Dec 1, 2006

Closed Book and Notes	No Calculators	Data Sheet Provided MET 320

R = 1.987 cal/K•gmole = 8.31 J/K•gmole

F = 23,060 cal/volt•gram equivalent = 96,259 cal/volt•gram equivalent

- Dry ice (solid CO2) is so named because it never melts at atmospheric pressure.  Its vapor pressure is above 1 atm at its melting point so it is long sublimated before melting.  The vapor pressure of dry ice is 5.11 atm at its melting point (-56.6 ºC, 216.4 K) and drops to 1 atm at (-78.5 ºC, 194.5 K).  Determine the heat of sublimation for dry ice from these data.

# Use the attached Ellingham Diagram for the problems below.

# (Show your work and submit the Ellingham Diagram.)

- Show on the attached Ellingham Diagram

- The pressure of O2 in equilibrium with Ti and TiO2 at 800°C

- The H2/H2O ratio in equilibrium with Ti and TiO2 at 800°C

- The CO/CO2 ratio in equilibrium with Ti and TiO2 at 800°C

- Set up a reaction extent problem for

3H2 + N2 = 2 NH3  	         KEQ = 1.2                       PT = 5 atm

The table below shows the number of moles of each component initially.

| Species | Initial Moles |  |  |
| --- | --- | --- | --- |
| NH3 | 0 |  |  |
| H2 | 10 |  |  |
| N2 | 4 |  |  |
| total | 2 |  |  |

##### Refer to the data for the Al-Au system at the end of the exam for Problems 3 and 4

- What is the volume of one gmole of CO2 at 304 K and 219 atm, which is three times its critical pressure of 73 atm?

- a) 	Calculate the Gibbs energy change for the oxidation of pure, liquid Al with O2 at a pressure of

1x10-12 atm to form pure, solid Al2O3 oxide.   The temperature is 1338 K (1611 ºC).

2/3 Al(l)  +  O2(g) =  4/3 Al2O3 (s)     	G° 1338 K = -711,620 Joules/gmole O2

b)	Which direction does the reaction proceed if the Gibbs energy change is less than 0?