South Dakota School of Mines and Technology

Department of Materials Metallurgical Engineering

MET 320	HQ 4	Dec. 5, 2011

SEE DATA SHEET AT END OF EXAM

NO CALCULATORS – CLOSED BOOK AND NOTES

If a problem seems to be in error, state the trouble, state an assumed correction, and proceed.

1.	The Cu in a liquid Ag-Cu solution at 1423 K and a composition of XCu = 0.3 reacts with O2 at 12 atm to form pure, solid Cu2O.  Show how to calculate the Gibbs energy change, ∆G, for this process.

DATA:

2 Cu(l) + 0.5 O2(g)  =  Cu2O(s)     	∆G°= -195,000 -7.12TlnT +143T J/gmole

Activity data for liquid

Ag-Cu Alloys at 1423 K

XCu 	aCu

0.0	0.000

0.1	0.260

0.2	0.422

0.3	0.535

0.4	0.616

0.5	0.679

0.6	0.731

0.7	0.782

0.8	0.841

0.9	0.912

1.0	1.000

2.	How many degrees of freedom are there in a system consisting of

the pure solids: MgO(s) , MgCO3(s) , CaO(s), CaCO3(s) and the gases: CO2(g), and N2(g)?

3. 	Fill in the blank.

| To obtain in a binary alloy | Given | Use Method or Equation |
| --- | --- | --- |
| The Integral Molar Quantity | The Partial Molar Quantities |  |
| The Partial Molar Quantity #1 | The Partial Molar Quantity #2 |  |
| Both Partial Molar Quantities | The Integral Molar Quantity |  |

- Show how to find the activity of Au in a liquid Al-Au alloy at 1338 K that is 60 atomic percent Au using the below Integral Molar Gibbs Energy of Mixing.

5.	How much heat would be expected from mixing

- 2 moles of liquid Al at 1338 K and 8 moles of liquid Au at 1338 K?

- 1 mole of liquid Al at 1338 K and 1,000,000 moles of liquid Al-Au alloy of XAl = 0.7 at 1338 K?

Data for Problem 5 (Cont’d on next page)

DATA from Hultgren, et al.  All G and H data are in calories.  All S data are in calories/K

Continues on the next page

- Short answer

- What is the difference between G and Gº?

- What is the relative partial molar heat of mixing for an ideal solution?

- What is the definition of the activity coefficient, i?

- A regular solution has an excess entropy of mixing of __________________________

- Circle the letters the denote solutions that observe Darken’s Quadratic Formalism:
 a,  b,  c,  d.

- On the below figure, show the areas corresponding to ln 1 and to ln 2 at X1 = 0.3.

Scratch Paper - discard

# Text boxes

0.0000035

ln 1

0

a

(1-X1)2

b

c

d

W

X2

0

1

0