SOUTH DAKOTA SCHOOL OF MINES AND TECHNOLOGY

DEPARTMENT OF METALLURGICAL ENGINEERING

MET 422	FINAL EXAM	Dec 19,1994

open book

All needed physical constants are to be obtained from the text.  Estimations are permissible if a needed constant is not available in the text.

1.	Find the drag force in dynes for a tethered sphere pulled through water.  The room-temperature water is flowing past the 2 cm. diameter sphere at 500 cm/sec.  The viscosity of water is 1 cP.

2.	The mass transfer coefficient km for forced convection is given by the function

km = f(V,r,h,D,DA)

Show that the Nusselt number for mass transfer is a function of Re and Sc by dimensionless analysis.

3.	The continuous vacuum degassing and casting arrangement shown below must provide 30,000 Kg/hr of molten steel to the strand caster.  The fluid level in the degasser must be kept at 2 meters depth.  The pressure inside the degasser is 0.0001 atm.  Show how to calculate the diameter of the nozzle.  The wall thickness is 30 cm.  Show all work and reference all required figures and equations.  rFe=7.8 g/cm3

4.	Estimate the rate of energy radiation through a 1 m x1 m charging door of an electric arc furnace with 50 cm thick walls operating at 1600 K.

5.	A steel cube 1 ft on an edge and at uniform temperature of 800 ¡C is withdrawn from a furnace and air cooled in a blowing stream with a temperature of 30 ¡C.

a)	Determine the temperature at the center of the cube after 1 hour for the following conditions:

h = 25 BTU/hr-ft2-¡F

k = 10 BTU/hr-ft-¡F

r = 490 lbm/ft3

Cp = 0.165 BTU/lbm-¡F

All six faces are cooled.  Ignore radiation

b)	How would the above solution differ if the cube were placed on a perfectly insulating surface of zero heat capacity so that heat would be removed from only five surfaces?

6.	Uniformly sized spherical drops of liquid lead are dropped down a shot tower through which cool air is blown upward as shown below.  The flow of air past the droplet is turbulent.

a)	What figure in the text would be needed to calculate the terminal velocity of the droplet?

b)	Assume the droplet's temperature is uniform and T0 when it reaches its terminal velocity.  Describe how to calculate the rate of heat transfer from the surface.  Be thorough.

7.	An electric heating element for a furnace is connected to the electric power source at each end by water-cooled clamps as shown below.  The rod's temperature is a function of the distance along the axis.  There are no significant radial gradients.  The electric power generates heat within the element at a rate of S Watts/cm3.  HEAT IS LOST FROM THE SURFACE AT THE RATE OF h(T-Tair) PER UNIT AREA OF SURFACE.  Derive an equation for the axial temperature profile in a rod L in length.  Since the temperature profile will be symmetrical about the center of the rod's axis, put your coordinate at the rod's center.  The rod's length is 2L and its radius is R.