OPEN BOOK

MET 422	HQ 2	Nov 19, 2008

1.	A composite flat wall is composed of the materials given in the table below.  Also given is each material’s thickness and thermal conductivity.  How many kilowatts would be lost through such a wall if it has an area of 10 m2 and an air temperature differential across it of 1000 degrees C?  The heat transfer coefficient on both sides is 20 Wm-2K-1.

| Table 1. Composite wall data |
| --- |
| Material | Thickness, m | k , W m-1 K-1 |
| Chrome Brick | 0.10 | 2.0 |
| Fire Brick | 0.20 | 1.0 |
| Insulating Brick | 0.40 | 0.5 |

- A 10-cm diameter horizontal aluminum cylinder at 200 °C is held motionless in cold dry air at 100 °C.  What is the rate of heat loss from each one meter length of the cylinder?

- Choose either a or b: Circle your selection. Only a will be graded unless your election of b is clearly marked or only b is attempted.

  - Set up the IN – OUT + GEN = ACC terms for a derivation of  the steady-state temperature profile for a rod of length L and diameter D that is held at TL at x = L, loses no heat in the x direction at x = 0, but loses heat by convection from its radial surface as shown. Write the BC’S.

  - Derive the differential equation for 2D USS HC in Rect coordinates with a generation term.

4.	A 20x20x200-cm steel specimen at 25 °C is suspended in a hot furnace at 825 °C.  Determine the temperature at the center of the specimen after 5 minutes.  Use ONLY the following data for your computations.

Data (more data are given than needed to solve the problem)

h	=	200 	Wm-2K-1	steel	=	7,900 	Kg m-3

ksteel	=	40 	W m-1K-1	kair	=	0.04 	W m-1K-1

Cpsteel	=	504 	J Kg-1K-1	Cpair	=	1000 	J Kg-1K-1

Prair	=	0.7		MWair	=	28.8

# Text boxes

q = h(T-Ta)

T = TL

qx = 0

x = L

x = 0