South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

# Met 426/526	HQ 1	March 8, 2002

Reference Data are attached.  Clearly include (show) with your work all data used from the reference sheets.  A Show all work in the space provided.  Turn in no other paper.

1.	Find ∆G° at 1873 K for the change in standard state for the reaction.

Ni(l)	=	Ni(1 wt % in Fe)

- What is the pressure of CO gas in equilibrium with Fe and Fe3O4 at 1000 K?  Assume total pressure of CO, CO2, and O2 is 1 atmosphere.

- What CO to CO2 ratio would be required to achieve an equilibrium wt% C of 0.4  at 1000 ºC?  Assume that fC = 1.

4.	Refer to Figure 2 below.

- Do the data for the Fe-Ni system at 1873 K conform to Darken’s quadratic formalism?  Why or why Not?

- It seems that the data for the Fe-Ni system could reasonably be interpreted to conform to lines A or B.  Here is a question about the consequences of choosing line A or B.

Which line would result in an interaction coefficient of Ni in Fe of zero and why?

  - Work a or b:  If both are attempted and your choice is not clear, “a“ will b graded.

- What is the mathematical relationship between the slope on a Darken Plot at infinite dilution and the Interaction Coefficient, .

- Describe the topochemical reduction of a single pellet using Ohm’s Law.  There is no need to describe each resistance in detail but driving force must be detailed.   Include a sketch (drawing).

  - Optional Bonus question that may be used to replace lost points above.  (10 points - above are 20 each.)

Derive an equation from which one could find the partial molar heat of mixing  at xi = 0 if the standard Gibbs energy change for the component going from pure liquid to the 1 wt%  standard state is

Go = a + bT

Table 1. Solution Thermodynamic Properties of the Liquid Fe-Ni System at 1873 K. (ref: Hultgren, Desai, Hawkins, Glieser, and Kelly, Selected Values of the Thermodynamic Properties of Binary Alloys, ASM, Metals Park, Ohio, 1973, p.852.)

| xNi | aFe | Fe | aNi | Ni |
| --- | --- | --- | --- | --- |
| 0.0 | 1.000 | 1.000 | 0.000 | 0.617 |
| 0.1 | 0.897 | 0.996 | 0.068 | 0.675 |
| 0.2 | 0.794 | 0.992 | 0.138 | 0.692 |
| 0.3 | 0.693 | 0.990 | 0.209 | 0.697 |
| 0.4 | 0.587 | 0.978 | 0.285 | 0.721 |
| 0.5 | 0.470 | 0.941 | 0.373 | 0.745 |
| 0.6 | 0.343 | 0.858 | 0.481 | 0.802 |
| 0.7 | 0.218 | 0.726 | 0.614 | 0.877 |
| 0.8 | 0.116 | 0.581 | 0.756 | 0.945 |
| 0.9 | 0.045 | 0.454 | 0.888 | 0.987 |
| 1.0 | 0.000 | 0.355 | 1.000 | 1.000 |

## Table 2.  Molecular Weights

| Element | MW |
| --- | --- |
| Ni | 58.70 |
| Fe | 55.85 |

Figure 1. Activities in the Liquid Fe-Ni System at 1873 K.

Figure 2. Darken Plot for the Liquid Fe-Ni System at 1873 K.

# Text boxes

A