# Integrated Steel Mills in the United States

As global technology improves, and becomes more and more integrated into the various sectors many aspects of the steel industry advance as well. These advancements are helping to blaze a trial into a new era of faster and more efficient processes.  The decline of large integrated mills and the rise of smaller, less expensive mini-mills is evidence of this.  The integrated steelmaking process begins in some integrated mills by producing “coke” from bituminous coal in what is called a coke oven. Coke is a solid carbonaceous residue derived from low-ash, low-sulfur bituminous coal. The volatile constituents of the coal (including water, coal-gas and coal-tar) are driven off by baking in an airless oven at temperatures as high as 1,000 degrees Celsius so that the fixed carbon and residual ash are fused together. Bituminous coal must meet a set of criteria for use as coking coal, determined by particular coal assay techniques. These include moisture content, ash content, sulphur content, volatilte content, tar and plasticity.

Coke is used as a fuel and as a reducing agent in smelting iron ore in a blast furnace. Coke from coal is grey, hard, and typically has the following properties:

- Specific Gravity of 1.85 – 1.9

- Porous

- A mass of coke is about 40% greater in volume then its coal equivilant.

- Heating value of 28 megajoules/kilogram.

As a side note, coke is not only produced from bituminous coal but can also be produced as an end byproduct of petroleum refinement. This type is sometimes termed “gas house coke”.

Once the the coal or petroleum has been refined and the coke produced, it is loaded into a furnace along with sinter, and limestone.  Sinter is produced by heating iron ore, fines, pellets, scale, etc. to bind them together. This mixture is then blasted with preheated air from below to promote the formation of pig iron. The pig iron, which is more dense, settles to the bottom while the lighter impurities such as sulfur-iron compounds, known as “slag” separates to the top.  The slag material is then poured off the top leaving the desired “pig iron” left which consists primarily of carbon-iron and pure iron.  The pig iron is then poured into a steel furnace and blown with pure oxygen to further remove impurities.

# The number of mills which take in iron ore and ship out a finished steel have fallen to just 25 plants by 1998, 11 of which are located near the Great Lakes.  These are owned by 15 steel and iron producing companies, some of which also operate non-integrated plants at the same locations.  In 1998 the Basic Oxygen Process was used to make 54.1 million tons of steel.  The use of this process represented 54.9 % of the total steel production in the United States, down from 56.2 % in 1997.   In the 1990’s companies running integrated mills have focused more upon specialty steels, particularly hot dipped galvanized, to ensure that automobile manufacturers continue using steel as the material of choice.

# Figure 1.  Integrated Steel Mill Flow

# There are 21 plants in the U.S. using blast furnaces to produce liquid iron 14 of which surround the Great Lakes.  They are shown below.

The industry has improved greatly from 100 years ago, and not just with respect to the processes it uses.  Safety, cleanliness, and environmental problems have all been dealt with to some degree and in many cases are one of the top priorities in today’s industry.  In 1998 there were 10 fatalities in the iron and steel industries, compared to hundreds of injuries and deaths each year around the turn of the century and that figure continues to decrease.

# Sources

# Iron and Steel. U.S. Geological Survey, Mineral Commodity Summaries, January 1998 http://minerals.usgs.gov/minerals/pubs/commodity/iron_&_steel/index.html

- Kesler, Stephen. Mineral Resources, Economics and the Environment, New York: Macmillan College Publishing Company, Inc.

- Liebman, Mark. “Ask the Expert” American Metal Market Online.  Online. January 22, 2000.   http://www.amm.com/ref/askmlieb.htm

- Wikipedia the free encyclopedia http://en.wikipedia.org/wiki/Steel_mill  This page was last modified 13:17, 30 January 2006

# Table 1.  Blast Furnace Locations, Capacities, and Injections

| Company | Location | Blast Furnaces Annual Total Capacity (t/year) | Injection (C = Coal, O = Oil, G = N. Gas) |
| --- | --- | --- | --- |
| ACME Steel | Chicago, IL | 1,400,000 | G |
| AK Steel | Ashland, KY | 2,000,000 | C,G |
| AK Steel | Middletown, OH | 2,300,000 | G |
| Bethlehem Steel | Chesterton, IN | 5,000,000 | C,G |
| Bethlehem Steel | Sparrow Point, MD | 3,450,000 | G |
| DSC Ltd. | Trenton, MI | 1,000,000 | G |
| Geneva Steel | Vineyard, UT | 3,300,000 | C,O,G |
| Gulf States Steel | Gadsden, AL | 1,100,000 | G |
| ISPAT Inland Steel | East Chicago, IN | 5,450,000 | C,G |
| LTV Steel | Cleveland, OH | 4,200,000 | O,G |
| LTV Steel | East Chicago, IN | 3,320,000 | O,G |
| National Steel | Granite City, IL | 1,770,000 | G |
| National Steel | Ecorse, MI | 3,700,000 | G |
| Rouge Steel | Dearborn, MI | 2,800,000 | G |
| US Steel | Braddock, PA | 2,300,000 | G |
| US Steel | Fairfield, AL | 2,300,000 | C,G |
| US Steel | Gary, IN | 7,750,000 | C,O,G |
| USS / Kobe Steel | Lorain, OH | 2,600,000 | C,G |
| WCI Steel Inc. | Warren, OH | 1,300,000 | G |
| Weirton Steel | Weirton, WV | 3,420,000 | O,G |
| Wheeling-Pittsburgh Steel | Steubenville, OH | 2,300,000 | G |

# Table 2.  Basic Oxygen Furnace Plants and Locations

| Company | Location |
| --- | --- |
| ACME Steel | Riverdale, IL |
| AK Steel | Ashland, KY |
| AK Steel | Middletown, OH |
| Allegheny Ludlum | Brackenridge, PA |
| Bethlehem Steel | Sparrows Point, MD |
| Bethlehem Steel | Chesterton, IN |
| Geneva Steel | Provo, UT |
| Gulf States Steel | Gadsden, AL |
| Inland Steel | East Chicago, IN |
| LTV Steel | Cleveland, OH |
| LTV Steel | East Chicago, IN |
| McLouth Steel Products | Trenton, MI |
| National Steel | Granite City, IL |
| National Steel | Ecorse, MI |
| Rouge Steel | Dearborn, MI |
| US Steel | Fairfield, AL |
| US Steel | Braddock, PA |
| US Steel | Gary, IN |
| USS / Kobe Steel | Lorain, OH |
| WCI Steel | Warren, OH |
| Weirton Steel | Weirton, WV |
| Wheeling-Pittsburgh Steel | Steubenville, OH |

# Text boxes

Basic Oxygen Furnace

Blast Furnace

Continuous Caster

Hot Strip Mill

Pickling

Cold Strip Mill

Coating Line

Anneal

Temper Mill

Coke Oven

Sinter Plant

Iron Ore

Coal

Final Products Shipped