Deborah Carlson

Met 426 Steelmaking

January 31, 2006

# Mini Mills

### History, Production, and Capacity

Mini mills are steel production facilities that convert steel scrap into the desired steel alloys using the electric-arc process to melt the scrap metal.  The electric-arc process involves placing electrodes above the steel scrap and striking an arc between the electrodes and scrap, which melts the scrap metal.  This process is beneficial due to its low capital cost and its use in areas with high amounts of steel scrap.  Since around 1945 the process has become more widespread for steel production.

The past twenty to thirty years has seen a great increase in the number of mini mills compared to integrated mills.  In 1970, steel production from mini mills was less than 10% of the total steel produced in the US.  Production from these mills was between 100,000 to 300,000 tons per year.  The production from mini mills has increased so much that by 2001 the mini mills produced nearly half of all the steel in the US.1  Worldwide in 2004, there were 65 mini mill steel producers, compared with 69 integrated mill producers.

Steel produced by the electric-arc process has steadily been increasing as shown in the graph below.  The data is from 1970 through 1990 and shows the percentage of steel produced through this process.

Figure 1.  Percentage of steel produced by the electric-arc process from 1970 to 1990 in the United States.

The production capacity of mini mills has also increased since the 1970s.  Now, they typically produce anywhere from 200,000 to 400,000 tons per year, however some plants can produce up to 3,000,000 tons per year.   Annual production for Nucor Corporation is given in the following table.

## Table 1.  Annual Production for Nucor Corporation4

| Production (tons per year) | Mini mill type | Number of plants | Average capacity of plants (tons per year) |
| --- | --- | --- | --- |
| 9,100,000 | Sheet mill | 4 | 2,275,000 |
| 6,700,000 | Bar mill | 10 | 670,000 |
| 2,100,000 | Plate mill | 2 | 1,050,000 |

Because of the advantages the electric-arc process and mini mills have over integrated mills, the production from these mills has steadily been increasing.  The capacity and production of mini mills has been increasing, as mini mills have proven to be an effective way to produce steel.

# Endnotes

References:

Young, Bob.  “Steel Mini Mills: A Recycling Success Story.”  Silicon Chip.  13 February 2002 <http://www.siliconchip.com.au/cms/A_30633/article.html>.

Smith, W.F.  “Carbon Steels.”  Structure and Properties of Engineering Alloys.  pg 86.

“Steel Producers.”  SteelVillage.com  2004  <http://www.steelvillage.com/steel.cfm?Category=24&newCategory=1&newHeading=Companies>.

“Iron and Steel Statistical Compendium.”  United States Geological Survey.  1990  <http://minerals.usgs.gov/minerals/pubs/commodity/iron_&_steel/stat/tbl2.txt>.

“Steel Mills: Mini Mills.”  Wikipedia: The Free Encyclopedia.  30 January 2006 <http://en.wikipedia.org/wiki/Steel_mill>.