# HOT-ROLLED STEEL PRODUCTION

## Up until the 1960’s, integrated steel mills accounted for all of the manufactured steel products in the country1.  The products made can generally be divided into two groups:

## long products (ex. Rods, bars, wire, structural, rails, pipe, tube, etc.), and

## flat products (ex. plate, hot rolled and cold rolled products)

Currently, approximately 70% of all manufactured steel come in the form of flat products.  Flat products, to this day, remain for the most part as the product of integrated steel mills.

A large portion of finished steel products is produced from hot rolling applications.  Basic operations in the hot rolling method takes a steel slab heated to elevated temperatures and shaped to a desirable size.  Temperatures at which the steel slab enters the rolling process are usually on the order of 2200( F and exit the process at approximately 1300( F 2,1.

The result of hot rolling applications can be seen all around us.  Examples resulting from the hot rolling process are rails, concrete reinforcement bars, and the automobile industry to name a few.  Because hot rolling products are so popular in the role they play in society, an increase in price came along over the span of 40 plus years.

This is evident in table one.

Table 1

Annual Average Hot-Rolled Steel Bar Price

(Dollars per one hundred pounds1)

Year 	Price	Year 	Price 	Year 	Price 	Year 	Price

1897 	0.99 	1923 	2.33 	1949 	3.35 	1975 	11.43

1898 	0.95 	1924 	2.20 	1950 	3.47 	1976 	11.32

1899 	1.95 	1925 	2.04 	1951 	3.70 	1977 	12.68

1900 	1.61 	1926 	1.99 	1952 	3.78 	1978 	14.01

1901 	1.44 	1927 	1.84 	1953 	4.05 	1979 	14.01

1902 	1.58 	1928 	1.87 	1954 	4.22 	1980 	16.20

1903 	1.56 	1929 	1.92 	1955 	4.47 	1981 	16.95

1904 	1.33	 1930 	1.73 	1956 	4.81 	1982 	17.23

1905 	1.48 	1931 	1.63 	1957 	5.25 	1983 	20.25

1906 	1.51 	1932 	1.58 	1958 	5.35 	1984 	22.08

1907 	1.60 	1933 	1.64 	1959 	5.68 	1985 	24.10

1908 	1.48 	1934 	1.81 	1960 	5.68 	1986 	24.10

1909 	1.31 	1935 	1.80 	1961	 5.68	 1987	 17.12

1910 	1.43 	1936 	1.92 	1962 	5.68 	1988 	17.25

1911 	1.26 	1937	 2.40 	1963	 5.74 	1989	 19.60

1912 	1.25 	1938 	2.35 	1964	 5.93 	1990 	20.43

1913 	1.38 	1939 	2.19 	1965 	5.93 	1991 	20.60

1914 	1.15 	1940 	2.15 	1966 	5.89 	1992 	17.48

1915 	1.31 	1941 	2.15 	1967 	5.92 	1993 	18.44

1916 	2.48 	1942 	2.15 	1968 	6.14 	1994 	18.95

1917 	3.49 	1943 	2.15 	1969 	6.56 	1995 	18.95

1918 	2.89 	1944	 2.15 	1970 	6.98 	1996	 18.95

1919 	2.43 	1945 	2.21	 1971	 7.89	 1997	 19.75

1920 	2.99 	1946 	2.47 	1972 	7.13 	1998 	18.75

1921	 1.89	 1947	 2.72 	 1973 	 8.38

1922 	 1.70 	 1948 	 3.09 	 1974 	10.78

1 To convert to dollars per metric ton, multiply by 22.0462.

Note:

1897-February 1987, hot-rolled carbon steel bars merchant, Pittsburgh base, dollars per cwt., in American Metal Market.

March 1987-1998, hot-rolled carbon SBQ (special bar quality) 1000 series, in American Metal Market.

### Bibliography:

- http://strategis.ic.gc.ca/SSG/mm01289e.html

2.) http://minerals.usgs.gov/minerals/pubs/commodity/iron_& _steel/350798.pdf Iron and Steel by Michael Fenton Annual Average Hot- Rolled Steel Bar Price (Dollars per one hundred pounds) 35 1992 dollars 30 Current dollars 25 20 15 10 5 0 1959 1962 1965 1968 1971 1974 1977 1980 1983 1986 ... http://minerals.usgs.gov/minerals/pubs/commodity/iron_& _steel/350798.pdf - size 28.0K hot: 7, rolled: 8, production: 3, 2.)hot rolled...: 8

3.) http://steel.org/learning/flowline/page2.htm