Temperature Dependence of Go for change to 1 wt% Standard State

For the reaction

Si(l) = Si		(1)

where i represents Si.

The temperature dependence of the activity coefficient is given by the Gibb’s-Helmholtz Equation as follows:

(2)

which gives

(3)

Integrating this and evaluating the constant of integration at 1873 K where is generally known (for steel making reactions) gives

(4)

where

that when substituted into Eq. (1) gives the desired result.

(5)

(6)

(7)