# Shaft Model Information

# Interstitial Velocity:   			Velocity of H2

= 0.35 void fraction

Gg = 0.005 gmoles*s-1*cm-2  		Superficial mole flux

T = 1000 K

Ggi = Gg/e =0.00175 gmoles*s-1*cm-2  	Interstitial mole flux

PV = nRT

dn/dt=Area*Ggi=Area*Gg/			Total Mole rate

dV/dt = RT/P * dn/dt  			Vol rate

dV/dt = Vel*Area

Vel = (dV/dt)/Area  			Gas velocity

Vel = RT*(dn/dt)/(P*Area)

Vel = RT*(Area*Gg/)/(P*Area)

Vel = RT*(Gg/)/P				Gas velocity (interstitial)

Vel =(82.03x1000)(0.0143)/1 =144 cm/sec

Unit check: (cm3*atm)K/(K*gfw)*(gfw)/(s*cm2)/atm [=]cm/sec