SOUTH DAKOTA SCHOOL OF MINES AND TECHNOLOGY

DEPARTMENT OF MATERIALS and METALLURGICAL ENGINEERING

Met 321	HQ 1	2/9/2001

Put all your answers on this sheet and the provided graph paper only.  Show condensed summaries of your work.  Scratch paper is allowed.

- Sketch a curve showing how the amount of a mineral resource changes with grade. (10)

- Sketch a curve showing the Mass of material used per unit Gross Domestic Product for a nation as a function of its per capita Gross Domestic Product. (10)

3.	Determine the degrees of freedom in the following systems:

a)	Solid CaCO3, CaO, CO2. (10)

b)	Add gaseous N2 to system (a). (5)

- Add solid MgCO3and MgO to system (a) - No N2. (5)

4.	List the data needed to calculate the activity from a phase diagram. (20)

- Describe in detail any method by which the partial molar heat of mixing of component 1 could be used to find the partial molar component of component 2.  Give equations.  Draw a sketch.  Show (algebraically) sample calculations. (30)

6.	Below is a plot of the integral molar heat of mixing for the A-B System.  Show on the plot how to obtain the partial molar heats of mixing for A and for B at . (10)

# Text boxes

0

1

0

XB

Grade

Reserves

Mass of material used per unit of Gross Domestic Product

per capita Gross Domestic Product