South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

Met 321	HQ 1	2/14/2003

- Questions on Cost, Conservation, and Concentration

a.	Sketch a curve showing how the amount of mineral resource changes with grade.

b.	Sketch a curve showing the Mass of material used per unit Gross Domestic Product for a nation as a function of its per capita Gross Domestic Product.

c.	Sketch the trend of inflation-adjusted unit cost of a typical metal during the 20th Century

d.	Sketch the total amount of Cu (as elemental including compounds) on Earth over the 20th Century

2.	Determine the degrees of freedom in each of the following systems:

a)	Solid austenitic Fe, solid C, gaseous CO plus CO2 at a total pressure of 1 atm.

b)	What if a second phase of alpha Fe is added to system (a) above?

- The three solids: MgO, SiO2, and CaO at 1 atm

- A system at a fixed temperature and consisting of ZnS, ZnO, SO2, and O2.

- A Stability Diagram (also known as a Predominance Diagram) is being constructed for the hypothetical M-O-Cl system.  On the chart below, write the approximate, relative positions of each of the following condensed phases:

M	MO	MOCl	MCl

M2O	MO3	MOCl2	MCl2

4.	Refer to Problem #3.  Assuming the following phases are adjacent (i.e. in equilibrium), what is the slope of the line between

- M2O and MO3

- MOCl2	and MCl2

- M and MOCl

5.	Refer to the attached ternary Phase Diagram for the MgO - SiO2 - CaO (M, S, C) system.  Characterize a batch composition of  40 wt% M and 10 wt % S at

- 2200 °C

- 2000 °C

- 1800 °C

Show all your work on the following diagrams as indicated.  Use symbols for lengths.

a) 2200 °C

b) 2000 °C

c) 1800 °C

# Text boxes

Time

Amount

Increasing Grade

Reserves

Per capita Gross Domestic Product

Mass of material consumed per unit of Gross Domestic Product

Time

Unit Cost

Log PO2

Log PCl2