South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

Met 321	Final Exam (Special)	May 8, 2003

1.	What cell potential would be required to produce Mg(l) and Cl2(g)  from MgCl2(l)?  The activity of the MgCl2 is 0.5 relative to the pure liquid. The pressure of chlorine is 1.1 atm and the temperature is 1000 K.

2.	How much argon per ton (vol at STP) would be required to deoxidize a steel heat containing 0.4 wt% C and 0.005 wt% O to 0.0005 wt% O by sparging with argon?

3.	Refer to the below  M-S-A (MgO-SiO2-Al2O3) phase diagram and indicated bulk composition.

- What are the final three crystals?

- What is the order and temperature of the first appearance of the three crystals?

- What is the percentage liquid at 1800 C?

- What crystal(s) are present at 1800 C?

4	A stability diagram for the Ni-S-O system is to be drawn.  The vertical coordinate is Log PSO2 and the horizontal coordinate is Log PO2.  The condensed compounds present are Ni, NiS, NiSO4, Ni3S2, and NiO.  The gases present include S2, O2, SO2, and SO3.

i)  	Sketch the diagram showing the relative position of each compound.

ii)	Assuming the NiSO4 and the NiS phases are in equilibrium, what is the slope of the line between them?

iii)	What would be the slope of a line of constant SO3?

5)	What is the mass flux in (Kg/m2/sec) from pure liquid Pb at 800 K?

6)	Describe the Refining Ratio (Equation) and how compute it at infinite dilution for the Pb-Zn system at 800K.

7)	Lab Questions

- Draw a silica network and show the effect of MgO addition.

- How was the Pb phase formed in the fire assay?

- Write the mass balances to solve the following problem:

A zinc flotation concentrate, substantially pure ZnS is roasted to ZnO without fuel.  The roaster gases contain 6% SO2 and 1% SO3, balance N2 and O2.  Give the mass balances needed to calculate the quantity of dry air fed to the roaster in per ton of ZnS.

From Phase Diagrams for Ceramists: American Ceramics Society

DATA

Data at 1600°C.   All dissolved components are in liquid iron.

+ = CO(g)			K = 500

+ 2= SiO2(g)		K = 17052

H2(g) = 2H	  		 K1600 = 7.3 X 10-6

log fSi = 0.029 [% Si]		MW Si = 28.09	MW Fe = 55.85

Si(1) in iron			1873K = 0.00132

∆Gvalues are in cal/gmole

MgCl2(l) = Mg(l) + Cl2(g)		∆G°1000 K = 115,000 cal/gmole

Si(1) + 02(g) = Si02 (B-quartz)		∆G= - 226,500 + 47.50 T  cal/gmole

Fe(1) + 1/2 02(g) = Fe0(1)		∆G= -56,900 + 11.82T  cal/gmole

SO2 + 0.5 O2 = SO3			∆G= -94,600 + 89.37T  cal/gmole

0.5 O2(g) = 				∆G°  = -28,000 - 0.69T  (cal)

Interaction coefficients for iron melts at 1873 K

e= 0.15		e= -0.20

e= -0.45		e= -0.04	Assume other ’s are 1.0

Other Information

F = 23,061 cal/(volt*equiv)

R = 1.987 cal/gmole-K = 0.08205 L*atm/K*gmole

1 atm = 1.013X105 Pascals             1 Pascal= 1Newton/m2                1Newton = 1 Kg*m/sec2

Attachments

Pure Zn and Pb datasheet from Hultgren, et al.

Alloy Pb-Zn datasheet from Hultgren, et al.

All pressures in atm,  All energies in calories per gmole

# Text boxes

Bulk Comp