South Dakota School of Mines and Technology

Department of Materials and Metallurgical Engineering

Met 321	HQ 2	4/4/2007

Put all your answers on this sheet and the provided graph paper only.  Show condensed summaries of your work.  Scratch paper is allowed.

- What cell potential would be required to perform electrolysis on Al2O3 dissolved in liquid cryolyte (Na3AlF6) at 1000 K.  The liquid is saturated with pure, solid Al2O3 to

a) 	produce pure, liquid Al and O2 gas at 1 atm using inert anodes and cathodes such that the overall reaction is

Al2O3 = 2Al + 1.5 O2 ?

b)	produce pure, liquid Al and CO2 gas at 1 atm using pure solid, carbon anodes and cathodes such that the overall reaction is

Al2O3 + 1.5C = 2Al + 1.5 CO2?

- What standard state should be used for each component in determining the Standard Gibb’s Energy changes for the above reactions for the stated conditions so that all the activities, fugacities (pressures) are known from the specified information?

Al2O3 	______________

C	______________

Al	______________

O2	______________

CO2	______________

- Sketch an Iron Blast Furnace and

a)	Label 5 items

b) 	Describe the following

i) 	Hot Metal

- Hot Blast

- Iron Notch

- Burden

- Top Gas

- a) Given the following reduction schemes letter designations:

S   - 		Molten salt electrolysis

C   - 		Carbothermic reduction

Ma - 		Matte Smelting

Me -		Metallothermic Reduction

Assign the following metal a likely production method:

Ti ___		Fe___ 		Ca___		Cu___

Ni___ 		Mg__		Al___		W___

b)	What are the advantages of Matte Smelting over sulfide roasting to oxide followed by Carbothermic reduction?

- How might matte smelting be made more energy efficient?

- What is the Kroll Process?

- An alloy of liquid Ag-Cu alloy at 1400 K is placed in a vacuum.  The mole fraction of Ag is 0.01.

a)	What is the refining ratio for the Ag?

b)	Could the alloy be completely refined of the Ag?

c)	Estimate the mass flux from a surface of pure molten Sn at 1400 K in a vacuum.

| Data for Cd-Sn Alloys and pure Elements |
| --- |
| P pure Sn @ 1400K | 2.12x10-6 atm |
| P pure Cd @ 1400 K | 19.02 atm |
| Activity Coef for Sn at infinite in Cd Dilution | 1.97 |
| Activity Coef for Cd at infinite in Sn Dilution | 1.69 |
| MW Sn | 118.7 |
| MW Cd | 112.4 |

1 atm = 101,300 Pa

5.	Lab Questions

a)	What is the value of Z called if Z is to1 mg as 31.14 g is to 2000 lbs?

- Why and How does the Pb form during the fusion step of the Au Fire Assay?

- If the oxygen bomb calorimeter temperature rises 5.4 F degrees with a 2400 grams water equivalent for the combustion of 1 gram of gasoline, estimate the fuel value of one gallon of gasoline.  (note: 6.3 lbs gasoline per gallon)

6.	a) Draw a silica network

b) Show how a basic component interrupts the silica network

7. 	Give the mass balances needed to calculate the quantity of dry air fed to the roaster.  Define all required quantities.  Set up the solution only.

Zinc sulfide, iron sulfide and lead sulfide concentrate composed of

40 moles  ZnS,

50 moles  PbS,

2   moles SiO2 (inert)

are to be roasted using oxygen-enriched  dry air containing 60% O2 and 40%N2.  No fuel is used.  The roaster gases contain 45% SO2, 5% SO3, balance N2.

DATA SHEET  - - Plus Ellingham Diagram

Data for the Pb-Zn system at 923 °K

| XZn | Zn | HMZn, Cal/gfw |
| --- | --- | --- |
| 0.2 | 4.709 | 3712 |
| 0.1 | 6.273 | 4293 |
| 0.0 | 7.94 | 4800 |

Data at 1600°C.   All dissolved components are in liquid iron.

+ = CO(g)			K = 500

+ 2= SiO2(g)		K = 17052

+ 2= SiO2(g)		K = 17052

H2(g) = 2H	  		K1600 = 7.3 X 10-6

log fSi = 0.029 [% Si]		MW Si = 28.09	MW Fe = 55.85

Si(1) in iron			1873K = 0.00132

∆Gvalues in cal/gmole

NaCl(l) = Na(l) + 1/2 Cl2(g)			∆G°  =  82,830

Si(1) + 02(g) = Si02 (B-quartz)			∆G°  = - 218,600 + 47.40 T

Fe(1) + 1/2 02(g) = Fe0(1)			∆G°  = -56,900 + 11.82T

SO2 + 0.5 O2 = SO3			∆G°  = -94,600 + 89.37T

0.5 O2(g) = 				∆G°  = -28,000 - 0.69T

H2(g) +0.5 O2(g) = H2O(l)			∆G°  298 K  = -57,500

Interaction coefficients for iron melts at 1873 K

e= 0.15;	e= -0.20;	e= -0.45;	e= -0.04;  Assume other fi's = 1.0

Other Information

F = 23,061 cal/v-equiv = 96,533 J/ v-equiv

R = 1.987 cal/gmole-K = 0.08205 L*atm/K*gmole

Vapor Pressure Data in atm, T[=]K:

,

, ,

Activity Coefficient Data for Al-Ag System

,