South Dakota School of Mines and Technology

# Department of Materials and Metallurgical Engineering

Met 321	HQ 3   60 points	5/4/07

1.	A vacuum-degassed steel contains 0.4 wt % carbon and is taken to a pressure of 10-5 atm at 1600°C.  Compute the equilibrium wt % O in the steel if

a) If fC is assumed to be 1.

b) If fC is not assumed to be 1 but computed using the interaction parameter.  (Data below)

2.	Rather than vacuum degassing the steel above it is decided to sparge it with argon to remove 99.9% of the oxygen. How many liters STP per ton would be needed?

3.	Find the standard Gibbs energy change for the following reactions:

a)  O2 (g at 1ATM) = O2 (g at 1PPM)          Go  = ?                           (1 PPM is meant to be 10-6 ATM)

b)  Cu (L, Pure) = Cu (1 wt% in Fe)          Go  = ?

DATA

Data at 1600°C.   All dissolved components are in liquid iron.

+ = CO(g)			K = 500

+ 2= SiO2(g)		K = 17052

H2(g) = 2H	  		 K1600 = 7.3 X 10-6

log fSi = 0.029 [% Si]		MW Si = 28.09	MW Fe = 55.85

Cu(1) in iron			1873K = 10.57	1873K = 9.512

Si(1) in iron			1873K = 0.00132	1873K = 0.0162

∆Gvalues are in cal/gmole

MgCl2(l) = Mg(l) + Cl2(g)		∆G°1000 K = 115,000 cal/gmole

Si(1) + 02(g) = Si02 (B-quartz)		∆G= - 226,500 + 47.50 T  cal/gmole

Fe(1) + 1/2 02(g) = Fe0(1)		∆G= -56,900 + 11.82T  cal/gmole

SO2 + 0.5 O2 = SO3			∆G= -94,600 + 89.37T  cal/gmole

0.5 O2(g) = 				∆G°  = -28,000 - 0.69T  (cal)

Interaction coefficients for iron melts at 1873 K

e= 0.15		e= -0.20

e= -0.45		e= -0.04	Assume other ’s are 1.0

Other Information

F = 23,061 cal/(volt*equiv)

R = 1.987 cal/gmole-K = 0.08205 L*atm/K*gmole

| Period | Group** |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1 IA 1A |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 18 VIIIA 8A |
| 1 | 1 H 1.008 | 2 IIA 2A |  |  |  |  |  |  |  |  |  |  | 13 IIIA 3A | 14 IVA 4A | 15 VA 5A | 16 VIA 6A | 17 VIIA 7A | 2 He 4.003 |
| 2 | 3 Li 6.941 | 4 Be 9.012 |  |  |  |  |  |  |  |  |  |  | 5 B 10.81 | 6 C 12.01 | 7 N 14.01 | 8 O 16.00 | 9 F 19.00 | 10 Ne 20.18 |
| 3 | 11 Na 22.99 | 12 Mg 24.31 | 3 IIIB 3B | 4 IVB 4B | 5 VB 5B | 6 VIB 6B | 7 VIIB 7B | 8 | 9 | 10 | 11 IB 1B | 12 IIB 2B | 13 Al 26.98 | 14 Si 28.09 | 15 P 30.97 | 16 S 32.07 | 17 Cl 35.45 | 18 Ar 39.95 |
|  |  |  |  |  |  |  |  | ------- VIII ------- ------- 8 ------- |  |  |  |  |  |  |  |  |
| 4 | 19 K 39.10 | 20 Ca 40.08 | 21 Sc 44.96 | 22 Ti 47.88 | 23 V 50.94 | 24 Cr 52.00 | 25 Mn 54.94 | 26 Fe 55.85 | 27 Co 58.47 | 28 Ni 58.69 | 29 Cu 63.55 | 30 Zn 65.39 | 31 Ga 69.72 | 32 Ge 72.59 | 33 As 74.92 | 34 Se 78.96 | 35 Br 79.90 | 36 Kr 83.80 |
| 5 | 37 Rb 85.47 | 38 Sr 87.62 | 39 Y 88.91 | 40 Zr 91.22 | 41 Nb 92.91 | 42 Mo 95.94 | 43 Tc (98) | 44 Ru 101.1 | 45 Rh 102.9 | 46 Pd 106.4 | 47 Ag 107.9 | 48 Cd 112.4 | 49 In 114.8 | 50 Sn 118.7 | 51 Sb 121.8 | 52 Te 127.6 | 53 I 126.9 | 54 Xe 131.3 |
| 6 | 55 Cs 132.9 | 56 Ba 137.3 | 57 La* 138.9 | 72 Hf 178.5 | 73 Ta 180.9 | 74 W 183.9 | 75 Re 186.2 | 76 Os 190.2 | 77 Ir 190.2 | 78 Pt 195.1 | 79 Au 197.0 | 80 Hg 200.5 | 81 Tl 204.4 | 82 Pb 207.2 | 83 Bi 209.0 | 84 Po (210) | 85 At (210) | 86 Rn (222) |
| 7 | 87 Fr (223) | 88 Ra (226) | 89 Ac~ (227) | 104 Rf (257) | 105 Db (260) | 106 Sg (263) | 107 Bh (262) | 108 Hs (265) | 109 Mt (266) | 110 --- () | 111 --- () | 112 --- () |  | 114 --- () |  | 116 --- () |  | 118 --- () |

Periodic Table: Ref: http://pearl1.lanl.gov/periodic/default.htm